## Slide 1: Hemp Reinforcement for Improved Strength of Wood Sodium Silicate Composites for Additive Manufacturing
-Nagendra Tanikella
Major Professor
Dr. Michael Maughan
Committee
Dr. Armando McDonald,
Dr. Daniel Robertson,
Dr. Ahmed Ibrahim
Funding: National Science Foundation

## Slide 2
The construction industry faces a dual crisis of environmental impact and economic unaffordability
2020 Global Status Report for Buildings and Construction Sector | UNEP - UN Environment Programme
https://www.axios.com/2022/06/07/housing-affordability-collapse

## Slide 3
Lumber mills convert only about 40% of wood volume to lumber
40%
60%
https://www.shutterstock.com/image-photo/tree-log-forest-pine-softwood-lumber-2664366591?
https://www.illinoisrealtors.org/wp-content/uploads/2020/06/house-frame-1200x630-1.jpg
https://pikbest.com/backgrounds/wood-image-an-of-pulp-and-chips_9441013.html

## Slide 4
Wood residues are being utilized at a lower-level

## Slide 5
Our solution combines sustainable materials (wood waste) with an additive manufacturing process (AM)
2024 Global Status Report for Buildings and Construction Sector | UNEP - UN Environment Programme
https://www.3dnatives.com/de/groesstes-3d-druckgebaeude-der-welt-qatar-100720251/

## Slide 6
The method involves using a single screw extruder connected to a custom 3D printer

## Slide 7
The baseline formulation is 40-mesh wood fibers with sodium silicate (WSSC) in a 50-50 ratio (dry basis)
Property | Typical WSSC values
Compression strength | 15-20 MPa
Tensile strength | 5-6 MPa
50-50
https://doi.org/10.1177/16878132231210373
https://www.flinnsci.com/sodium-silicate-solution-4-l/s0103/

## Slide 8
Concrete is reinforced with steel rebar for tensile strength and aggregates for cost/compression strength
https://www.ecc-edu.net/en/service/tutoring/details/reinforced-concrete-2
https://www.shutterstock.com/image-photo/contractors-lay-down-area-storage-precast-98231729

## Slide 9
Hemp is a rapidly renewable plant that requires less water, and land and produces more, stronger fibers than cotton
https://doi.org/10.1007/s10570-022-04583-w
Hemp hurd
Hemp fiber

## Slide 10
The research is structured as three studies to develop an optimized, high-strength composite
Study 1. Feasibility of short hemp fiber reinforcement
Study 2. Incorporation of hemp hurd
Effect of particle size
Study 3. Continuous hemp fiber reinforcement
Tensile strength
Extrudability and printability
Compression and flexural strength
Optimization based on cost, strength, extrudability
Modification of the die

## Slide 11
Study 1: Sodium silicate, hemp fiber amount and lengths were varied for experimental design
Variable materials | Levels
Sodium silicate (SS) (wt%): | 45-55
Hemp fiber (wt%): | 2.5-10
Hemp fiber (HF) lengths (mm): | 1-5

## Slide 12
Longer fibers and low sodium silicate lead to processing issues and high motor power
Motor power (W) | Average extrusion time (min)
> 90 | 34
< 90 | 25
1 mm
5 mm
Clumps of fiber

## Slide 13
How did the factors affect motor power and viscosity?

## Slide 14
How did the factors affect motor power?

## Slide 15
How did the factors affect motor power?
0.314
0.539
0.01
p-values

## Slide 16
How did the factors affect strength?

## Slide 17
How did the factors affect strength?

## Slide 18
Hemp fiber amount was the significant factor for improving mechanical strength

## Slide 19
Chart: Strength (MPa)
| Flexural strength | Compression strength
0% Hemp fiber | 16.64 | 14.828
5 wt% hemp fiber | 21.8296 | 20.108
The formulation with 5% hemp fiber of 3 mm length, 50% sodium silicate was selected for 3D printing test
31%
36%

## Slide 20
Study 2: Hemp hurd, sodium silicate were varied, along with the wood fibers for experimental design
Factor | Levels/Values
Hemp hurd (HH) (wt%) | 0-15
Hemp fiber (HF) (wt%) | Fixed at 5 (3 mm length)
Sodium silicate (SS) (wt%) | 50-60, 50 + 5Water
Wood fiber Type (WFT) | Unsifted, 40 mesh, pellet

## Slide 21
Wood fibers were sifted using a 40-mesh screen

## Slide 22
Wood pellets were ground using a coffee grinder before use

## Slide 23
Materials used in this study

## Slide 24
How did the factors affect strength and density?

## Slide 25
Finer particles result in stronger, denser composites

## Slide 26
Finer particles resulted in stronger, denser composites

## Slide 27
How did the factors affect motor power and viscosity?

## Slide 28
High motor power was observed with small particle sizes at low sodium silicate amounts

## Slide 29
High motor power was observed with small particle sizes at low sodium silicate amounts

## Slide 30
Strength-cost analysis for all formulations

## Slide 31
Strength-cost analysis, after formulations with high motor power are removed

## Slide 32
Strength-cost analysis for pellets and 40 mesh wood fibers

## Slide 33
Two formulations showed high strength-to-cost ratio, with low motor power

## Slide 34
Pellet-formulation is stronger, but 40 mesh-formulation is lower cost

## Slide 35
The pellet-formulation uses less sodium silicate than the 40 mesh-formulation, for the same strength
Strength/SS: 0.891 MPa/g
Strength/SS: 0.869 MPa/g

## Slide 36
Pellets have a higher density than unpelleted wood fibers

## Slide 37
Pellets are preferable due to logistics

## Slide 38
Optimization of the formulation with hemp fiber and hurd reinforcement, and wood pellets replacement
32%
118%
29%

## Slide 39
Study 3: Die modification for continuous fiber reinforcement

## Slide 40
Critical length of a fiber is the length at which a fiber becomes maximally useful
https://doi.org/10.1088/1757-899X/508/1/012006

## Slide 41
Interfacial shear stress and critical length were measured using single fiber pullout test
Three treatment conditions:
No treatment
Water
Sodium silicate

## Slide 42
Interfacial shear stress and critical lengths were improved by sodium silicate treatment
Voids

## Slide 43
Tensile strength of composite was 60% higher with sodium silicate treated fiber
60%

## Slide 44
This dissertation improved the flexural, compression and tensile strength using multi-scale reinforcement
Increase in flexural, compression strengths by 75%, and strength/cost by 29%.
Novel method for continuous fiber reinforcement; increase in tensile strength by 60%, using 5 vol% hemp twine.

## Slide 45
Future work
Testing in real world conditions.
Complete cost analysis, including equipment, labor to compare with lumber/concrete construction.
Further improvement in tensile strength using higher fiber fractions.
Alternative bio-based resins.
Questions?